## Slide 1
RUNGTA COLLEGE OF DENTAL SCIENCES & RESEARCH
TITLE OF THE TOPIC: AMALGAM
DEPARTMENT OF CONSERVATIVE DENTISTRY AND ENDODONTICS

## Slide 2: Specific learning Objectives
Core areas* | Domain ** | Category #
COMPOSITION CLASSIFICATION OF AMALGAM | COGNITIVE | MUST KNOW
INDICATIONS ADVANTAGES METALLURGICAL PHASES | PSYCHOMOTOR | NICE TO KNOW
TERMONOLOGIES | AFFECTIVE | DESIRE TO KNOW
At the end of this presentation the learner is expected to know ;

## Slide 3: Table of Content
HISTORICAL BACKGROUND
CONSTITUENTS
CLASSIFICATION OF AMALGAM ALLOY
INDICATION AND CONTRAINDICATION
ADVANTAGES AND DISADVANTAGES
METALLURGICAL PHASES
DIMENSIONAL CHANGES
REFERENCES

## Slide 4: HISTORICAL BACKGROUND
Used as a dental restorative material from the beginning of the 19th century.
Amalgam was made by mixing mercury with the fillings from Spanish or Mexican silver coins (high silver content).

## Slide 5
TERMINOLOGY | DEFINITION
Amalgam | Amalgam is an alloy which has mercury as one of its components – Marzouk (1997)
Dental Amalgam | An alloy of mercury, silver, copper, tin, which may also contain palladium, zinc, and other elements to improve handling characteristics and clinical performance – Anusavice (2003)
Dental Amalgam Alloy / Alloy for Dental Amalgam | An alloy of silver, copper, tin, and other elements that is formulated and processed in the form of powder particles or as a compressed pellet – Anusavice (2003)

## Slide 6: Constituents of Amalgam
As per ADA Specification No. 1
Basic
  Silver
  Tin
  Copper
  Mercury
Others
  Zinc
  Indium
  Palladium

## Slide 7: Basic Constituents
Silver (Ag)
  Increases strength
  Increases expansion
  Decreases creep
Tin (Sn)
  Decreases expansion
  Decreases strength
  Reduces the resistance to tarnish
  and corrosion
Phillip’s Science of Dental Materials 2003

## Slide 8: Basic Constituents
Copper (Cu)
  Increases strength
  Reduces tarnish and corrosion
  Reduces creep
    reduces marginal deterioration
Phillip’s Science of Dental Materials 2003

## Slide 9: Basic Constituents
Mercury (Hg)
  Activates reaction
  Only pure metal that is liquid at room temperature
  Spherical alloys
    require less mercury
      smaller surface area easier to wet
        40 to 45% Hg
  Admixed alloys
    require more mercury
      lathe-cut particles more difficult to wet
        45 to 50% Hg
Phillip’s Science of Dental Materials 2003

## Slide 10: Other Constituents
Indium (In)
  Decreases surface tension
    reduces amount of mercury necessary
    reduces emitted mercury vapor
  Reduces creep and marginal breakdown
  Increases strength
  Must be used in admixed alloys
Powell J Dent Res 1989

## Slide 11: Other Constituents
Zinc (Zn)
  Used in manufacturing
    decreases oxidation of other elements
    acts as scavenger or deoxidizer
  Provides better clinical performance
    less marginal breakdown
  Causes delayed expansion with low Cu alloys
    if contaminated with moisture during condensation or trituration.
Phillip’s Science of Dental Materials 2003
H2O + Zn ZnO + H2
Þ

## Slide 12: Other Constituents
Platinum and Palladium (Pd)
  Reduces corrosion
  Hardens the alloy
Mahler J Dent Res 1990

## Slide 13: CLASSIFICATION OF AMALGAM ALLOYS
1. BASED ON COPPER CONTENT:
a) Low copper alloys : contains less than 6% of copper .
b) High copper alloys : contains more than 6% of copper.
-Admixed or dispersion alloys .
-Single composition alloys.
2. BASED ON ZINC CONTENT
a) Zinc containing alloys: contains less than 0.01% zinc
b) Non zinc/Zinc free alloys: contains equal to less than 0.01%

## Slide 14: COPPER CONTENT
Composition | LOW COPPER | HIGH COPPER |  | 
 |  | Admixed |  | Unicomposition
Particle shape | Lathe- Cut / Spherical | Lathe-cut (2/3) | Spherical (1/3) | Spherical
Silver | 63-70% | 40-70 % | 40-65 % | 40-60 %
Tin | 26-23 % | 26-30 % | 0-30 % | 22-30 %
Copper | 2-5 % | 2-30 % | 20-40 % | 13-30 %
Zinc | 0-2 % | 0-2 % | 0 % | 0-4 %

## Slide 15
3. BASED ON SHAPE OF ALLOY PARTICLES
  a) Lathe cut alloys –irregular shape.
  b) Spherical alloys
  c) Admix alloys
4. BASED ON NUMBER OF ALLOYED METALS
  a) Binary alloys – Ag Sn
  b) Ternary alloys – Ag Sn Cu
  c) Quaternary alloys- Ag Sn Cu In
5. BASED ON SIZE OF ALLOY
  a) Micro-cut
  b) Fine-cut
  c) Coarse cut

## Slide 16: INDICATIONS
- As permanent filling material in
  Class 1 and Class 2 cavities and
  Class 5 cavities where esthetics is not a prime
  consideration
  In combination with metallic retentive pins to restore a crown
  For making dies
  In retrograde root canal filling

## Slide 17: CONTRAINDICATIONS
Anterior teeth and clearly visible surfaces of posterior teeth.
Allergy to any component of amalgam, proven by skin test, conducted by trained dermatologist.
Patient’s with proven amalgam – induced lichenoid lesions.
Remaining tooth structure requires support / would require extensive preparation to accommodate amalgam.
Treatment of incipient / early primary fissure caries.

## Slide 18: ADVANTAGES
Easy to insert
Not overly technique sensitive
Maintain anatomical form
Adequate resistance to fracture
Prevent marginal leakage
Can be used in stress bearing areas
Relatively long service life

## Slide 19: DISADVANTAGES
Non esthetic
Brittle
Subject to corrosion and galvanic action
May show a degree of marginal breakdown
Do not help retain weakend tooth structure
Regulatory concerns about disposal of amalgam

## Slide 20: TAKE HOME MESSEGE/ FOR THE TOPIC COVERED (SUMMARY)
Dental amalgam are widely used by the dental profession in most parts of the world
Some countries like swedan, Canada and Germany, uk have either banned or imposed serious limitation on amalgam usage
The American dental association council on scientific affairs has conclude that both amalgam and composite materials are considered safe and effective for tooth restoration .

## Slide 21: Question & Answer Session
Students should be given opportunity to ask question for clarifying for their understand/ confusions. Teachers must spend 5-10 minutes for this to improve the output.

## Slide 22: REFERENCES
STURVEDANTS art and science of operative dentistry text book of operative dentistry NISHA GARG AND AMIT GARG

## Slide 23
THANK YOU