## Slide 1
RUNGTA COLLEGE OF DENTAL SCIENCES & RESEARCH
TITLE OF THE TOPIC: AMALGAM
DEPARTMENT OF CONSERVATIVE DENTISTRY AND ENDODONTICS

## Slide 2: Specific learning Objectives
Core areas* | Domain ** | Category #
COMPOSITION CLASSIFICATION OF AMALGAM | COGNITIVE | MUST KNOW
INDICATIONS ADVANTAGES METALLURGICAL PHASES | PSYCHOMOTOR | NICE TO KNOW
TERMONOLOGIES | AFFECTIVE | DESIRE TO KNOW
At the end of this presentation the learner is expected to know ;

## Slide 3: Table of Content
HISTORICAL BACKGROUND
CONSTITUENTS
CLASSIFICATION OF AMALGAM ALLOY
INDICATION AND CONTRAINDICATION
ADVANTAGES AND DISADVANTAGES
METALLURGICAL PHASES
DIMENSIONAL CHANGES
REFERENCES

## Slide 4: DIMENSIONAL STABILITY
Dimensional Change
  Severe contraction may lead to –
    Microleakage
    Plaque accumulation
    Secondary caries
  Excessive expansion may lead to –
    Pressure on pulp
    Post op.sensitivity
    Protrusion of restoration

## Slide 5
ANSI/ADA Specification No.1 requires that amalgam should neither contract nor expand more than 20 mm/cm, measured at 37 degree C, between 5 min and 24 hr after beginning of trituration.

## Slide 6: Dimensional Change
Most high-copper amalgams undergo a net contraction
Contraction leaves marginal gap
  initial leakage
    post-operative sensitivity
  reduced with corrosion over time
Phillip’s Science of Dental Materials 2003

## Slide 7: Dimensional Change
Net contraction
  type of alloy
    spherical alloys have more contraction
      less mercury
  condensation technique
    greater condensation = higher contraction
  trituration time
    overtrituration causes higher contraction
Phillip’s Science of Dental Materials 2003

## Slide 8: Effect of moisture contamination
If a zinc containing low copper or high copper amalgam is contaminated by moisture during trituration or condensation, a large expansion can take place
Expansion usually starts after 3-5 days and may continue for months reaching values greater than 400mm
DELAYED EXPANSION

## Slide 9
DELAYED EXPANSION | The gradual expansion of a zinc-containing amalgam over weeks to months, which is associated with hydrogen gas development caused by contamination of the plastic mass with moisture during its manipulation in a cavity preparation– Anusavice (2003)

## Slide 10: STRENGTH
Develops slowly
  1 hr: 40 to 60% of maximum
  24 hrs: 90% of maximum
Spherical alloys strengthen faster
  require less mercury
Higher compressive vs. tensile strength
Weak in thin sections
  unsupported edges fracture
Phillip’s Science of Dental Materials 2003

## Slide 11: STRENGTH
Effect of trituration
  Both undertrituration or overtrituration decreases strength
Effect of mercury content
  Strength – function of volume fractions of unconsumed alloy particles and mercury containing phases
  Use of low mercury/alloy ratio recommended

## Slide 12: STRENGTH
Effect of condensation
  Lathe cut alloys- greater the condensation pressure, higher the compressive strength
  Spherical alloys – lighter pressures produce adequate strength
Effect of porosity
Effect of amalgam hardening rate
  As per ANSI/ADA sp.1, minimum compressive strength of 80 Mpa should be achieved at 1 hr.

## Slide 13: Amalgam Properties
Compressive Strength (MPa)
Creep %
Tensile Strength
(24 hrs) (MPa)
Amalgam Type
1 hr
7 days
Low Copper1
145
343
2.0
60
Admixture2
137
431
0.4
48
Single Composition3
262
510
0.13
64
Phillip’s Science of Dental Materials 2003
1Fine Cut, Caulk 2 Dispersalloy, Caulk 3Tytin, Kerr

## Slide 14: CREEP
Creep | The time-dependent strain or deformation that is produced by a stress. The creep process can cause an amalgam restoration to extend out of the cavity preparation, thereby increasing its susceptibility to marginal breakdown. – Anusavice (2003)
Marginal Breakdown | The gradual fracture of the perimeter of margin of a dental amalgam restoration that leads to the formation of gaps or ditching at the external interfacial region between the amalgam and the tooth. – Anusavice (2003)

## Slide 15: CREEP
Slow deformation of amalgam placed under a constant load
  load less than that necessary to produce fracture
Correlates with marginal breakdown
  Higher the creep, greater is the degree of marginal deterioration
Phillip’s Science of Dental Materials 2003

## Slide 16: Influence of Microstructure on Creep
Creep rates
  Increase with higher 1 volume fraction
  Decrease with larger 1 grain sizes
  2 associated with higher creep rates
    Associated with  rods, which act as barriers to deformation of the 1 phase

## Slide 17
Amalgam Type | Creep %
Low Copper1 | 2.0
Admixture2 | 0.4
Single Composition3 | 0.13
Phillip’s Science of Dental Materials 2003
1Fine Cut, Caulk
2 Dispersalloy, Caulk
3Tytin, Kerr

## Slide 18: TAKE HOME MESSEGE/ FOR THE TOPIC COVERED (SUMMARY)
Dental amalgam are widely used by the dental profession in most parts of the world
Some countries like swedan, Canada and Germany, uk have either banned or imposed serious limitation on amalgam usage
The American dental association council on scientific affairs has conclude that both amalgam and composite materials are considered safe and effective for tooth restoration .

## Slide 19: Question & Answer Session
Students should be given opportunity to ask question for clarifying for their understand/ confusions. Teachers must spend 5-10 minutes for this to improve the output.

## Slide 20: REFERENCES
STURVEDANTS art and science of operative dentistry text book of operative dentistry NISHA GARG AND AMIT GARG

## Slide 21
THANK YOU