## Slide 1: RUNGTA COLLEGE OF DENTAL SCIENCES AND RESEARCH
DENTAL CEMENTS
DEPARTMENT OF CONSERVATIVE DENTISTRY AND ENDODONTICS

## Slide 2: Specific learning objectives at the end of this presentation the learner is expected to know ;
Core areas* | Domain ** | Category #
Introduction | Cognitive | Must know
classification | Cognitive | Must know
Compositions | Cognitive | Must know

## Slide 3: Contents
Introduction
Key terms
Agents for pulp protection
Ideal requirements
Classifications
Properties
composition

## Slide 4
Calcium Hydroxide cement
Composition :
Base paste:
Glycol Salicylate - 40% Reacts with Cal hyd &zinc oxide
Titanium dioxide- inert filler, pigments
Barium sulphate- radio opacity
Catalyst paste:
Calcium hydroxide- 50% principal reactive ingredient
Zinc stearate- accelerator
Setting Reaction
Calcium hydroxide reacts with salicylate ester to form chelate-amorphous calcium disaliscyate.
Setting time-2-5 minutes.

## Slide 5
Mode of supply:
1 two paste system
2 single paste system
3 light cured system
Manipulation :
Equal lengths of two pastes are dispensed on paper pad & mixed to a uniform colour
Light activated Calcium hydroxide Cement
Light activated cements consists of calcium hydroxide& barium sulphate dispersed in urethane dimethacrylate
It also contains HEMA & polymerization activators .
It has long working time & is less brittle

## Slide 6
Properties:
Low compressive strength-10 to 27 Mpa
Low tensile strength-1Mpa
Thick layers provide thermal insulation
Solubility in water is high
Cement is alkaline-Ph –range 9.2—11.7
Helps in formation of reparative dentin

## Slide 7
Uses:
1. Direct pulp capping,
2. Indirect pulp capping,
3. Pulpotomy ,
4. Apexogenesis,
5. Apexification
6. Low strength sub- bases under composite restorations for pulp protection
7.Intracanal medicament
8.As a root canal sealer
9.Treatment of perforation ,internal ,external resorption.

## Slide 8: Take home message
It is type of direct restorative material which may be defined as the substance that hardens to act as base, liner, filling material, or adhesive to bind devices and prostheses to tooth structure or to each other. Dental cements used as restorative materials have low strengths compared with those of resin-based composites and amalgam.

## Slide 9: Questions
Define dental cements
What are different classification of dental cements ?
Give composition of different cements ?

## Slide 10: Suggested reading
Basic dental materials by manappallil
Philip’s science of dental sciences

## Slide 11
Thank you