## Slide 1: RUNGTA COLLEGE OF DENTAL SCIENCES AND RESEARCH
DENTAL CEMENTS
DEPARTMENT OF CONSERVATIVE DENTISTRY AND ENDODONTICS

## Slide 2: Specific learning objectives at the end of this presentation the learner is expected to know ;
Core areas* | Domain ** | Category #
Introduction | Cognitive | Must know
classification | Cognitive | Must know
Compositions | Cognitive | Must know

## Slide 3: Contents
Introduction
Key terms
Agents for pulp protection
Ideal requirements
Classifications
Properties
composition

## Slide 4: Zinc Polycarboxylate cement
In the quest for an adhesive luting agent that can bond strongly to tooth structure, zinc polycarboxylate evolved as the first cement system that developed an adhesive bond to tooth structure.
Applications:-
1. Primarily for luting permanent restorations
2. As bases and liners
3. Used in orthodontics for cementation
Mode of supply:-
Powder and Liquid in bottles
Powder which is mixed with water
Pre-capsulated powder/liquid system.

## Slide 5: Composition
Powder
Zinc oxide- Basic ingredient
Magnesium oxide- principal modifier and aids in sintering
Other oxides like bismuth
and aluminum ……. Small amounts
Stannous Flouride….. Increases strength, modifies setting
time, and imparts anticariogenic
properties.

## Slide 6: Liquid
Aqueous solution of polyacrylic acid
or
Copolymer of acrylic acid with other carboxylic acids
i.e., Itaconic, Maleic, or tricarboxylic acid- 32% to 42% by weight.

## Slide 7: Setting Reaction
the powder and Liquid are mixed
The surface of the powder particles are attacked by the acid releasing Zinc, Magnesium and Tin ions.
These released ions bind to the polymer chain via the cross linked salts.
Structure of set cement:-
The set cement consist of an amorphous gel matrix of zinc polycarboxylate in which unreacted powder particles are dispersed.
Setting time:- 7 to 9 minutes.

## Slide 8: Properties:-
Mechanical Properties:-
Compressive strength- 55Mpa
It is inferior to Zinc phosphate cement.
Tensile strength- 6.2Mpa
its tensile strength is slightly higher than that of Zinc phosphate cement.
Solubility and Disintegration- 0.06%
It tends to absorb water and is slightly more soluble than zinc phosphate.
The marginal dissolution of cement is more when used as cementing medium.

## Slide 9
Biocompability:-
They are less irritant to the pulp than Zinc phosphate because…
1. The pH rises more rapidly than Zinc phosphate.
2. penetration of polyacrylic acid into the dentinal tubules is less because of its higher molecular weight and larger size.
Adhesion
the cement bonds chemically with the tooth structure.
This is due to the ability of the carboxyl group in the polymer molecules to chelate with calcium in the tooth structure.
Adhesion is better to smooth surface
Does not adhere to Gold or Porcelain.
Optical properties
Thermal Properties
They are good thermal insulators.

## Slide 10: Manipulation
1. the tooth surface should be meticulously cleaned using 10% polyacrylic acid solution followed by rinsing with water.
2. 1.5 parts of powder to 1 part of liquid by weight.
3. the mixing is done on paper pad
4. the liquid is taken just prior to mixing
5. the powder is incorporated into the liquid in large quantities
with stiff agate spatula.
6. The remaining powder is added to adjust the consistency.
7. the mixing should be completed in 30-45 seconds.
8. the cement should be used while the surface is still glossy.
9.Remove the excess cement only when it has hardened.

## Slide 11: Take home message
It is type of direct restorative material which may be defined as the substance that hardens to act as base, liner, filling material, or adhesive to bind devices and prostheses to tooth structure or to each other. Dental cements used as restorative materials have low strengths compared with those of resin-based composites and amalgam.

## Slide 12: Questions
Define dental cements
What are different classification of dental cements ?
Give composition of different cements ?

## Slide 13: Suggested reading
Basic dental materials by manappallil
Philip’s science of dental sciences

## Slide 14
Thank you