## Slide 1: RUNGTA COLLEGE OF DENTAL SCIENCES AND RESEARCH
DENTAL CEMENTS
DEPARTMENT OF CONSERVATIVE DENTISTRY AND ENDODONTICS

## Slide 2: Specific learning objectives at the end of this presentation the learner is expected to know ;
Core areas* | Domain ** | Category #
Introduction | Cognitive | Must know
classification | Cognitive | Must know
Compositions | Cognitive | Must know

## Slide 3: Contents
Introduction
Key terms
Agents for pulp protection
Ideal requirements
Classifications
Properties
composition

## Slide 4
Zinc silicophosphate cement
Has resulted from combination of zinc phosphate cement & silicate powders
A.D.A. specification -21
Type 1 cementing medium
Type 2-temporary posterior filling material
Type 3- both uses
Anticariogenic due to Fl release
High compressive strength- 165 Mpa.
Semitransluscency
Uses-luting agent
intermediate restorations
As a die material.

## Slide 5
Resin cements
They are filled & unfilled resins
Supply – powder & liquid system
- two paste system
Setting 4-10 min
reaction – chemical [ peroxide –amine induction ]
-light activation
Enamel bonding by acid etch
Dentin bonding by dentin bonding agents
Irritant to pulp
Insoluble in oral fluids
Use cementation of porcelain veneers ,crowns& bridges

## Slide 6
Copper cement
Copper oxide ,[cuprous –red, cupric –black]
Zinc oxide
they are bacteriostatic & bactericidal
irritant to pulp-Ph 5.3
USES:
Temporary fillings in children
Inermediate restorations

## Slide 7: Zinc Oxide- Eugenol Cement
These cements have been used extensively since-1890’s.
In general ,they are cements of low strength.
Depending on their use they vary widely in their properties.
Least irritating of all dental cements.
Known to have Obtundant effect on exposed dentin.

## Slide 8
Classification:-
According to ADA specification no-30
Type I- For temporary cementation
Type II- For permanent cementation
Type III- Temporary filling material and thermal insulation
Type IV- Cavity liners.
Mode of supply:-
It is available in two forms
1. Powder and Liquid
2. Two paste system

## Slide 9: Composition
Powder
Zinc oxide- 69.0% Principal ingredient.
White rosin- 29.3% to reduce brittleness of set cement.
Zinc Stearate- 1.0% Accelerator, Plasticizer
Zinc acetate- 0.7% Accelerator, improves strength.
Magnesium oxide- is added in some powder. it acts with
eugenol in similar manners as zinc oxide.

## Slide 10
Liquid:-
Eugenol- Reacts with zinc oxide
Olive oil- Plasticizer
Setting Reaction:-
When the powder and liquid are mixed
In the first phase of reaction hydrolysis of zinc oxide to its hydroxide takes place
Water is essential for the reaction to proceed.
The reaction proceeds as a typical acid-base reaction to form a chelate.
The chelate forms amorphous gel that tends to crystallize imparting strength to the set mass.
Structure of set cement:-
The set cement consists of particles of zinc- oxide embedded in
A matrix of particles of zinc eugenolate.
Setting time- 4 to 10 minutes.

## Slide 11
Factors affecting setting time
Manufacture:-
The most active zinc oxide powders are those formed by decomposing zinc salts like zinc hydroxide and zinc carbonate by heating at 300°C
Particle size- smaller particles set fast
Accelerators- Alcohol, glacial acetic acid,
Heat- accelerates setting
Retarders- Glycol and Glycerine.
Powder to Liquid ratio- the higher the ratio, the faster the set

## Slide 12
EBA alumina modified cements
These were introduced in an effort to improve mechanical properties of zinc oxide eugenol cement.
Powder:
Zinc Oxide - 70%
Alumina - 30%
Liquid:
EBA- 62.5%
Eugenol- 37.5%
Compressive strength increased-55Mpa
They have longer working times,
setting time-9.5 minutes.

## Slide 13
Polymer reinforced ZnOE (IRM)
Zn Oxide powder is surface treated, the combination of surface treatment and polymer reinforcement results in..
good strength
improved abrasion resistance
toughness
effective seal
Composition
Powder:-
Zinc oxide
Finely divided natural or
Synthetic resins

## Slide 14
Liquid
Eugenol
Acetic acid- accelerator
Thymol - antimicrobial agent.
Setting time- 6 to 10 minutes
Properties
Cements have improved properties
1.Compressive strength- 48 Mpa
2.Tensile strength- 4.1 Mpa
3.Modulus of elasticity- 2.5 Gpa
4.Film thickness- 32 um
5.Solubility &Disintegration- 0.03% wt
6. Pupl response- moderate.

## Slide 15: Take home message
It is type of direct restorative material which may be defined as the substance that hardens to act as base, liner, filling material, or adhesive to bind devices and prostheses to tooth structure or to each other. Dental cements used as restorative materials have low strengths compared with those of resin-based composites and amalgam.

## Slide 16: Questions
Define dental cements
What are different classification of dental cements ?
Give composition of different cements ?

## Slide 17: References
Basic dental materials by manappallil
Philip’s science of dental sciences

## Slide 18
Thank you